**************************************************************************

USACE / NAVFAC / AFCEC	UFGS-06 17 19 (November 2016)

Change 2 - 05/21

Preparing Activity: USACE	New

UNIFIED FACILITIES GUIDE SPECIFICATIONS

References are in agreement with UMRL dated April 2025

**************************************************************************

SECTION 06 17 19

CROSS-LAMINATED TIMBER

11/16, CHG 2: 05/21

************************************************************************** NOTE:	This guide specification covers the

requirements for fabrication and erection of cross laminated timber panels for walls, floors, roofs, partitions, and all metal shapes and hardware required for their installation. Cross-Laminated  Timber (CLT)	is prefabricated engineered wood  products made of at least three orthogonal layers of  graded sawn lumber or structural composite lumber  (SCL) that are laminated by gluing with structural  adhesives. The term "cross laminated timber"  comprises suitably selected and prepared layers of  lumber bonded together with adhesives, the grain of  which is oriented in accord with engineered wood  specifications, typically with every other layer set  perpendicularly to each other.

Adhere to UFC 1-300-02 Unified Facilities Guide Specifications (UFGS) Format Standard when editing this guide specification or preparing new project specification sections.	Edit this guide specification for project specific requirements by adding, deleting, or revising text.	For bracketed items, choose applicable item(s) or insert appropriate information.

Remove information and requirements not required in respective project, whether or not brackets are present.

Comments, suggestions and recommended changes for this guide specification are welcome and should be as a Criteria Change Request (CCR).

**************************************************************************

PART 1	GENERAL

************************************************************************** NOTE:	Cross laminated timber (CLT) is an engineered

wood building system used to complement light-and heavy-timber framing options. Layers of lumber are

laminated together in alternating directions to form a solid wood panel with high strength and dimensional stability.	Typical lay-ups use an odd number of layers, resulting in a primary and secondary structural axis. Manufactured panels are typically 2.40.6 to 3 m 82 to 10 feet wide, up to 510

500 mm 20 inches thick, and up to 20 m 64 feet

long.	75 percent lighter than concrete, they can be used as an economical alternative to concrete slabs, masonry and steel in many building types. The manufacturing process has been standardized, but the panels are fabricated as needed to custom dimensions.

**************************************************************************

************************************************************************** NOTE:	Include in the drawings:

Details of all panels, showing cross sections and dimensions.

Include in designs, engineered wood specifications including bending strength (Fb) and Modulus of Elasticity (E ) for Laminated Veneer Lumber, and Fb and grading. 	Specifications

to use National Design Standards.

Assumed loads, including floor live load, roof live load, wind load, and concentrated loads (partitions, and equipment mounted on or suspended therefrom).

Layout, showing location of laminated members and floor elevations, and identification of Appearance Grades.

Details of hangers for suspended ceilings, pipes, light fixtures, or other construction, as required. The preferred method is to request detailed shop  drawings from the manufacturer/installer.

Details of metal shapes and hardware required for connections. Preferred method is to request detail  shop drawings from the manufacturer/installer.

Pressure preservative treatment for protection  against decay and insects in accordance with AITC

109.	It should be incorporated into specification  when wet use conditions prevail. CLT cannot be  pressure treated, at this time, because of its large size. Avoid  its use in wet conditions. Other wood products that  are pressure treated in accordance with AITC 109 can  be used instead, where necessary.

**************************************************************************

  - REFERENCES

************************************************************************** NOTE:	This paragraph is used to list the

publications cited in the text of the guide specification.	The publications are referred to in the text by basic designation only and listed in

this paragraph by organization, designation, date, and title.

Use the Reference Wizard's Check Reference feature when you add a Reference Identifier (RID) outside of the Section's Reference Article to automatically place the reference in the Reference Article.	Also use the Reference Wizard's Check Reference feature to update the issue dates.

References not used in the text will automatically be deleted from this section of the project specification when you choose to reconcile references in the publish print process.

**************************************************************************

The publications listed below form a part of this specification to the extent referenced.	The publications are referred to within the text by the basic designation only.

Some referenced standards and criteria for Glued-Laminated Wood are being applied to Cross-Laminated Timber (CLT) as a similar material by reference in this section.

# AMERICAN INSTITUTE OF STEEL CONSTRUCTION (AISC)

AISC 360	(20162022) Specification for Structural Steel Buildings

# AMERICAN SOCIETY OF CIVIL ENGINEERS (ASCE)

ASCE 7-22	(2022; Supp 1 2023; Supp 2 2023) Minimum Design Loads and Associated Criteria for Buildings and Other Structures

# AMERICAN SOCIETY OF MECHANICAL ENGINEERS (ASME)

ASME B18.6.1	(2016) Wood Screws (Inch Series) AMERICAN WOOD COUNCIL (AWC)

AWC NDS	(20182024) National Design Specification (NDS) for Wood Construction

# APA - THE ENGINEERED WOOD ASSOCIATION (APA)

ANSI/APA PRG 320	(20122019) Standard for Performance Rated Cross-Laminated Timber

ANSI/APA 405	(2023) Standard for Adhesives for Use in  Structural Laminated Timber

APA EWS T300	(20072023) Technical Note: Glulam Connection Details

# ASTM INTERNATIONAL (ASTM)

ASTM A36/A36M	(2019) Standard Specification for Carbon Structural Steel

ASTM A123/A123M	(2024) Standard Specification for Zinc  (Hot-Dip Galvanized) Coatings on Iron and  Steel Products

ASTM A276/A276M	(2024) Standard Specification for Stainless Steel Bars and Shapes

ASTM A666	(2023) Standard Specification for Annealed or Cold-Worked Austenitic Stainless Steel Sheet, Strip, Plate and Flat Bar

ASTM A1011/A1011M	(2023) Standard Specification for Steel Sheet and Strip, Hot-Rolled, Carbon, Structural, High-Strength Low-Alloy, High-Strength Low-Alloy with Improved Formability, and Ultra-High Strength

ASTM F1667/F1667M	(2021a) Standard Specification for Driven  Fasteners:	Nails, Spikes, and Staples

FPInnovations (FPI)

SP-529E	(2013) CLT Handbook, Cross-Laminated Timber (U.S. Edition)

# INTERNATIONAL CODE COUNCIL (ICC)

ICC IBC		(2024) International Building Code INTERNATIONAL ORGANIZATION FOR STANDARDIZATION (ISO)

ISO ISO/IEC 17020	(2012) Conformity Assessment - Requirements for the Operation of Various Types of Bodies Performing Inspection

ISO ISO/IEC 17065	(2012) Conformity Assessment - Requirements for Bodies Certifying Products, Processes and Services

  - SUBMITTALS

************************************************************************** NOTE:	Review Submittal Description (SD) definitions

in Section 01 33 00 SUBMITTAL PROCEDURES and edit the following list, and corresponding submittal items in the text, to reflect only the submittals required for the project.	The Guide Specification technical editors have classified those items that require Government approval, due to their complexity or criticality, with a "G."	Generally, other submittal items can be reviewed by the Contractor's Quality Control System.	Only add a "G" to an item, if the submittal is sufficiently important or complex in context of the project.

For Army projects, fill in the empty brackets following the "G" classification, with a code of up to three characters to indicate the approving

authority.	Codes for Army projects using the Resident Management System (RMS) are:	"AE" for Architect-Engineer; "DO" for District Office (Engineering Division or other organization in the District Office); "AO" for Area Office; "RO" for Resident Office; and "PO" for Project Office. Codes following the "G" typically are not used for Navy and Air Force projects.

The "S" classification indicates submittals required as proof of compliance for sustainability Guiding Principles Validation or Third-Party Certification and as described in Section 01 33 00 SUBMITTAL PROCEDURES.

**************************************************************************

Government approval is required for submittals with a "G" or "S" classification. Submittals not having a "G" or "S" classification are for Contractor Quality Control approval, and are for information only.	 When used, a code following the "G" classification identifies the office that will review the submittal for the Government. Submit the following in accordance with Section

# 01 33 00 SUBMITTAL PROCEDURES:

SD-03 Product Data

Custom Finishes; G, [	] SD-04 Samples

Exposed-To-View Surfaces; G, [	] SD-05 Design Data

Installation Drawings SD-07 Certificates

AITC Quality Mark or APA-EWS Trademark Cross-Laminated Timber Panels Conformance Certification

SD-08 Manufacturer's Instructions Erection Procedures

Handling

# QUALITY ASSURANCE

    - Qualifications for Cross Laminated Timber (CLT) Manufacturer

Provide panels that meet ANSI/APA PRG 320 standards, factory produced by an American Institute of Timber Construction (AITC) or APA - The Engineered Wood Association (APA) licensed manufacturer.	Factory mark every panel with AITC Quality Mark or APA-EWS trademark and provide a certificate of conformance.	Marks must not be visible in final assembly.

Manufacture of the panels must conform to AWC NDS and FPI SP-529E.

      - Preinstallation Conference: Conduct conference at Project site.

        - Attendees: Installer and representatives of manufacturers and  fabricators involved in or affected by the installation and its  coordination or integration with other materials and  installations that have preceded or will follow.

        - Notify Owner’s representative, AOR, SEOR and testing agency of  scheduled meeting dates.

    - Certifications

Submit certificates for cross-laminated timber panels.	Include a product report or laboratory report issued by a U.S. product certification agency accredited under ISO ISO/IEC 17065 or a U.S. product inspection agency accredited under ISO ISO/IEC 17020.	Include the following information in the certification:

      - CLT Manufacturer's Standards

      - CLT stress grade and appearance classification

      - Lay-up of wood, species and grades used

      - Connection Hardware Standards in accordance with CLT Manufacturer's specifications

      - Manufacturer's panel durability tests and testing results

Ensure material tested is typical of a production run of the same material used in the project.	Conduct tests on the same production lot(s) for delivery of the panels.

Manufacturer must be qualified and certified.

- Certification: Manufacturer of CLT shall be pre-qualified to  manufacture panels certified in accord with ANSI/APA PRG 320.

- Design Standards: Manufacturer shall comply with National Design  Specification (NDS) for Wood Construction.

    - Surfaces

Submit three samples, each of 100300 millimeters 412 inches minimum square by three laminate thickness for industrial grade faced product and 300 millimeters 12 inches square by three laminate thickness sample for visual/architectural grade panels to illustrate the quality and color of exposed-to-view surfaces.

# DELIVERY, STORAGE, AND HANDLING

Deliver the panels to the project site in covered or protected systems in accordance with manufacturer's standards or recommended instructions for proper handling and storage and contractor's weather and moisture  protection plan.	Label and deliver in sequence of construction for the project, equipped with loading straps by the manufacturer, erected by

certified crane operators and fabrication handlers and protected for prolonged inclement weather conditions after erected.	Replace any damaged or deteriorated panels.

- ​Protect mass timber panels during delivery, storage and handling with  water-resistant covering, in accordance with Contractor’s Weather and  Moisture Protection Plan.

- Support units during shipment on non-staining material in same  position as during storage.

- Store units with adequate bracing and protect units to prevent contact  with soil and separated with stripping, so air may circulate around  all faces of mass timber panels. Take actions to prevent staining,  cracking, distortion, warping or other physical damage.

  - Handle and transport units in a position consistent with their  shape and design to avoid excessive stresses that would cause  cracking or damage. Protect corners with wood blocking.

  - Slit underside of weather-resistant membrane covering during  storage at site to avoid accumulation of condensation or  moisture. Take care to not deface underside surface of mass  timber panels.

  - If factory coverings have been removed, cover top and sides with  opaque moisture-resistant membrane.

Submit manufacturer's instructions for handling, erection procedures, sequencing, administration of screws and attachments and recommended tools and tolerances.	Note applicable safety precautions and standards.	Have a copy of all instructions present on the project site.

# PART 2	PRODUCTS

  - SYSTEM DESIGN

Verify all field measurements prior to preparation of fabrication and Installation drawings to ensure proper fitting of the work.

    - Drawings

Provide shop drawings and installation drawings for CLT panels showing sequence of placement, location, sizes, overall dimensions, reinforcement, screw and attachment locations, safe handling directions and any special erection instructions.	Include any reinforcement necessary for safe handling and erection of panels.	Identify each panel and the corresponding sequence and procedure followed during installation, and location and details of anchorage devices that are embedded in other construction on layout drawings.

    - Shop Drawings

Supplier shall provide [two-dimensional, three-dimensional/BIM] shop  drawing submittal including the following information:

- Indicate member locations, orientation, elevations, and spacing. Label  each mass timber panel with a piece number or other unique mark.

- Indicate the location of structure and elements supporting the mass  timber panels. [Indicate slope of panels in installed position.]

- Indicate the size and shape of openings in mass timber panels,  positioned relative to gridlines in plan, and positioned relative to  floor levels in elevation.

- For each panel:

  - Show layout, dimensions, major strength direction, and elevations.

  - Clearly indicate layup type, CLT grade, appearance  classification, and shop finishes.

  - Clearly indicate lumber species and appearance requirements,  where that is requested in the design documents.

  - Include dimensioned details of cuts, openings, holes, fasteners,  and connection hardware.

  - Provide weight, center of gravity, and designated lift point  coordinates of each panel.

Shop drawing submittal can be combination of layout, installation, and/or  piece drawings.

    - Conformance Certification

Submit signed and sealed documentation prepared by a licensed professional [engineer] [architect] verifying conformance with ASCE 7-22, AWC NDS and ICC IBC standards.

# PERFORMANCE REQUIREMENTS

    - Structural Performance

CLT panels shall meet or exceed minimum design values required in Contract  Documents without exceeding design stresses, and deflection requirements  determined according to the applicable building code and the AWC NDS and  acceptable to authorities having jurisdiction.

The Contractor shall hire a registered design professional to author and  submit for record a written statement of the means and methods employed  for the installation and temporary support of CLT panels and supporting  structure during construction.

# MATERIALS

    - General

Provide CLT Panels fabricated in accordance with ANSI/APA PRG 320.

    - Cross Laminated Timber (CLT) Panels

Manufacturer shall have ANSI/APA PRG 320 certification for layups required  by Contract Documents.,

**************************************************************************

NOTE:	Specify required grades and layups of CLT for  Project. These can include “basic” grades and layups  defined directly in ANSI/APA PRG 320 as well as  manufacturer specific “custom” grades meeting  ANSI/APA PRG 320 standard. These can include CLT  made from solid sawn lumber as well as CLT made from  SCL, such as MPP. Acceptable CLT products can be  specified in the construction documents or in these  specifications.

**************************************************************************

CLT grade and layup requirements as specified in Structural Contract  Documents.

************************************************************************** NOTE:	OR

**************************************************************************

CLT Grade and Layup Requirements:

- CLT Grade and Layup: As agreed by AOR, SEOR and mass timber panel  manufacturer.

  - CLT Grade: [	]:

************************************************************************** NOTE:	Enter Grade from PRG 320 or Custom

Manufacturer Grade

**************************************************************************

  - Longitudinal Layer Lamination Grade: [	].

- CLT Layup: [	]:

************************************************************************** NOTE:	enter layup designation or description of

layup

**************************************************************************

  - Number of Layers: [Three] [Five] [Seven] [	].

  - Thickness of Layers: [	].

- Panel Thickness, Structural: [4.125 in.] [ 6.875 in.] [ 9.625 in.]  [	in.].

- Structural gluing of lamination edge joints is not required.

- Side pressing CLT during manufacturing [is] [is not] required.

Adhesives: Provide adhesive products in compliance with ANSI/APA PRG 320.

Any appearance classifications should be coordinated with manufacturers to  ensure specified requirements are achievable. See CLT Design Guides for  additional information.

************************************************************************** NOTE:	Designer should determine the species and

grade based on the design application and use, and

delete the non-applicable selections below.

Select the appropriate stress grade from ANSI/APA PRG 320 or describe in detail an alternative grading required. (ANSI/APA PRG 320 grades are not mandatory to meet the standard.	Alternative grading is allowed.)	When CLT is used as a floor slab, ensure a grade is selected for the span to limit deflection to l/480 or a maximum of 13 mm half of an inch.

Select one of the following appearance grades:

Architectural grade contains normal growth characteristics such as tight knots and medium seasoning checks.	All knot holes and voids over 19mm

3/4 inch are filled.

Industrial grade has a greater number of open defects, including knot holes.	Industrial grade is appropriate for industrial installations, floor beams, concealed construction, or other applications where appearance is not an important consideration.

**************************************************************************

      - Stress Grade

CLT panels must be [E1] [E2] [E3] [V1] [V2] [	] stress grade, graded in accordance with ANSI/APA PRG 320.

      - Appearance Classification

CLT panels must meet the [Architectural] [Industrial] appearance classification in accordance with ANSI/APA PRG 320.

        - Appearance Classifications for CLT of Lumber Laminations

Architectural Appearance Classification: For locations where mass timber  panels are indicated on the Construction Documents to meet the  Architectural Appearance Classification, the face layers exposed to view  shall meet the following requirements.

          - All knot holes and voids measuring over 3/4 inch (19 mm) are filled  with a wood-tone filler or clear wood inserts selected for similarity  with the grain and color of the adjacent wood.

          - The case layers exposed to view are free of loose knots and open knot  holes are filled.

          - Knot holes do not exceed 3/4 inch (19 mm) when measured in the  direction of the lamination length with the exception that a void may  be longer than 3/4 inch (19 mm) if its area is not greater than 1/2  inch2 (323 mm2).

          - Voids greater than 1/16 inch (1.6 mm) wide created by edge joints  appearing on the face layers exposed to view are filled.

          - Exposed surfaces are surfaced smooth with no misses permitted.

**************************************************************************

NOTE:	Following are requirements beyond those of  the Architectural Appearance Classification of PRG  320 Appendix X1 and can be included if desired and  coordinated with the manufacturer.

**************************************************************************

          - [Sanding: Sand surfaces indicated to be exposed to view in final  construction]

          - [Pitch Streaks: Pitch streaks are not permitted.]

          - [Wane: Wane on exposed panel face(s) is not permitted.]

          - [The corners of the panel exposed to view in the final structure shall  be eased with a minimum radius of 1/8 inch 3 mm or equivalent chamfer.]

************************************************************************** NOTE:	CLT grades from some solid sawn lumber

species groups allow for multiple species (e.g.,  Douglas-Fir and Larch) within a species group  (Douglas-Fir-Larch). Use this item if a specific  species is required for outer visible layer. Before  specifying a single species within a species group,  coordinate with the potential manufacturers to  verify what is achievable.

**************************************************************************

          - [Species of outer visible layer: <other value>.]

          - [<Enter further appearance requirements, per project requirements>.]

Industrial Appearance Classification: For locations where mass timber  panels are indicated on the Construction Documents to meet the Industrial  Appearance Classification, the face layers exposed to view shall meet the  following requirements:

- Voids appearing on the edges of laminations need not be filled.

- Loose knots and knot holes appearing on the face layers exposed to  view are not filled.

- Members are surfaced on face layers only and the appearance  requirements apply only to these layers.

- Occasional misses, low laminations or wane (limited to the lamination  grade) are permitted on the surface layers and are not limited in  length.

************************************************************************** NOTE:	The following are requirements beyond those

of the Industrial Appearance Classification of PRG  320 Appendix X1 and can be included if desired and  coordinated with the manufacturer.

**************************************************************************

- [Staining: Heart and/or blue stain are allowed up to 5 percent of  visual surface.]

- [Shake and Checks: Shall not exceed 36 inches or ¼ of panel length.]

- [<Enter further appearance requirements, per project requirements>.]

************************************************************************** NOTE:	The following requirements can apply to

panels that are not exposed to view and where no  appearance requirements are needed beyond the  structural grade requirements of the laminations  used in the panels.

**************************************************************************

Non-Visual Appearance Classification: For locations where mass timber  panels are [not indicated on the Construction Documents to meet any other  Appearance Classification][not exposed to view in the final construction],  the face layers exposed to view shall meet the following requirements:

- Shake and checks allowed, not limited.

- Heart wood and blue stain allowed, not limited

- Occasional misses, low laminations or wane (limited to the lamination  grade) are permitted on the surface layers and are not limited in  length.

- Knots (limited to the lamination grade) are permitted [ Custom Defined Appearance Grade:

- As agreed by AOR and mass timber panel manufacturer.

- <Enter further appearance requirements, per project requirements>.

]

        - Appearance Classifications for CLT of SCL Laminations

Architectural Appearance Classification of CLT of SCL laminations: For  locations where CLT of SCL laminations are indicated on the Construction  Documents to meet the Architectural Appearance Classification, the face  layers exposed to view shall meet the following requirements:

          - Exposed Panel Face: [Structural][Architectural] lamination to face of  CLT; rotary cut Douglas-Fir nominal 1/8-inch veneer. [G1

Plus][HD-face].

          - [Grade A Douglas-Fir, rotary cut], nominal 1/2-inch LVL, to visible  faces of CLT; sanded smooth and sealed.

************************************************************************** NOTE:	Retain if more qualify control is required

for faces. Verify availability with manufacturer.

**************************************************************************

          - [Provide void-free without splits and wane. Sort veneers as required.]

          - [Staining: Heart and blue stain are allowed, maximum 5 percent of  panel area.]

Industrial Appearance Classification: For locations where mass timber  panels are indicated on the C.

      - Moisture Content

Comply with ANSI/APA PRG 320 for moisture content, up to a maximum of 1516 percent, and compatible with the criteria of the certified adhesive applied.

[2.3.3	Preservative[ and Fire-Retardant] Treatment

************************************************************************** NOTE:	Include heading and following paragraphs when

fire-retardant treatment is required to achieve a  specified flame spread rating.	Fire-retardant  treatment is intended and recommended only for  interior use and in locations not subject to  alternate wetting or drying action.	AITC 109 and  APA S580 are for preservative treated wood  exclusively.

**************************************************************************

Wherever CLT is in the exterior of the conditioned building envelope; or in direct contact with the ground, building foundation, or concrete; or in damp or humid service conditions, use preservative treated wood.[		Treat exposed structural panels with a fire retardant to attain a UL flame  spread rating not greater than 25.]	Pressure impregnate [preservative]  [fire-retardant] treated wood with an approved process for the location in accordance with AITC 109 or APA EWS S580D, AWPA T1, and AWPA U1.	Any  strength or stiffness reduction due to treatment must be provided by the treater.	Kiln dry all wood after treatment to remove the moisture added during treatment.	Moisture content throughout material after drying must be less than 15 percent.

]2.3.3	Fire Resistant Ratings

Provide fire resistance test data or provide engineering judgments for the required fire resistance as shown on architectural drawings.

    - Adhesive

Adhesives must be certified by test for use with the species to which it is applied in accordance with ANSI/APA 405 and ANSI/APA PRG 320.	Apply and allow set times as required by the adhesive manufacturer's instructions.	Also, apply pressure on the panels and for the duration

during manufacture as required by the adhesive manufacturer's instructions. [2.3.5	Finishes

************************************************************************** NOTE: Delete this when finishes are not required.

Retain the following if a shop applied finish is  required.	Coordinate with manufacturer on what is  appropriate for the project.

The blank set of brackets allows specification of  color.

**************************************************************************

[No protective coating of the base panels is required.] [Submit custom  finishes as specified by the designer and applied by the factory or on  site.] [Provide cross-laminated timber members with standard factory wiped stain and clear varnish finish [as indicated by manufacturer's  designations] [match sample] [as selected from manufacturer's full range] [	]][Shop-Applied Edge Sealer:

      - Apply edge sealer to mass timber panels within an enclosed,  weather-protected finishing and storage space.

      - Apply [one coat][two coats] of penetrating type, clear, non-yellowing  end sealer [, compatible with specified finish coating] to all edges  of penetrations, holes, openings, and perimeter edges of mass timber  panels:

        - Basis-of-Design Product:	KP-12 UVW by Sansin Corp

        - Other Approved Products:	<TBD>.]

************************************************************************** NOTE:	Retain the following if a shop-applied

membrane is required. Coordinate with manufacturer  on what is appropriate for the project.

**************************************************************************

[Shop-Applied Weather Protection Membrane: <TBD>]

************************************************************************** NOTE:	Retain the following if a field-applied

finish is required.

************************************************************************** [Field-Applied Final Finish,[ Exterior][ and][ Interior] Applications:  Coordinate with final field-applied finish stain and seal in Section [09  91 00 “Painting”][09 93 00 “Staining and Transparent Finishing”][09 96 00  “High-Performance Coatings”]].

    - .1	Wrapping Material

Weatherproof and lightproof material to protect mass timber panels from  moisture and light damage.

      - Adhesive Sealing Tape at Panel Joints and Ends

For protection of mass timber panels from movement of water down through  mass timber system and from moisture at concrete during topping slab  placement and curing.

][2.3.6	Timber Hardware

************************************************************************** NOTE:	Delete this paragraph when timber hardware is

not required.

**************************************************************************

Design connections to AWC NDS, and AISC 360 unless specifically detailed by the Engineer of Record, to resist shears, moments and forces indicated.	Fabricate connective hardware in accordance with AISC 360.

Clean oil, dirt, rust, and foreign matter from all metal surfaces. Fasteners:

        - Steel Angles: [ASTM A36/A36M, galvanized per ASTM A123/A123M] [As  specified in Section 05 50 00 METAL FABRICATIONS].

        - Nails: Conform to ASTM F1667/F1667M.

        - Wood Screws: Conform to ASME B18.6.1.

        - Proprietary Self-Tapping Screws: Conform to third-party product  evaluation report from an approved agency.

[2.3.6.1	Structural Steel

Provide structural steel shapes, plates, and flat bars as indicated for assembly and connection of members conforming to ASTM A36/A36M.

][2.3.6.2	Hot-Rolled Steel Sheet

Provide hot-rolled steel sheet complying with ASTM A1011/A1011M, structural steel, Type SS, Grade 33.

][2.3.6.3	Stainless Steel

[ Provide stainless steel bars and shapes complying with ASTM A276/A276M [Type 304] [Type 316].

][Provide stainless steel plate, flat bars, and sheets complying with ASTM A666 [Type 304] [Type 316].]

# ]]PART 3	EXECUTION

  - PREPARATION

Clean oil, dirt, rust, and foreign matter from all metal surfaces.

# INSTALLATION

Conform to spacing and placement of panels and installation methods in accordance with the manufacturer's instruction and APA EWS T300.	Provide close fits and neat appearance of joints without binding or adding additional stresses to the panel.	Hoist panels in place in accordance with the manufacturer's instructions using non-marring straps and connectors. Brace erected member to maintain a safe working environment and stable structure.

Avoid on-site cuts; however, if necessary, only with the approval of the designer or engineer of record, except for fastener drilling and other minor cutting.	Coat all cuts and inside surfaces of drilled holes with end sealer.

# EXAMINATION

Prior to site erection, examine site conditions and ensure acceptable  conditions for erection.

Examine locations to receive mass timber panels, with Installer present,  for compliance with requirements, installation tolerances, and other  conditions affecting performance of the Work.

Proceed with installation only after unsatisfactory conditions have been  corrected.

# PREPARATION

Bracing and Temporary Shoring: Follow installation method statement and

bracing plan, including evaluation of temporary loading conditions and  bracing of structure during installation.

# INSTALLATION

General: Comply with installation method statement and bracing plan.

Erect mass timber panels in accordance with engineered rigging plans and  in coordination with reviewed shop drawings.

Follow Project’s Weather and Moisture Protection Plan throughout  construction period, until building is enclosed.

Make adequate provision for possible erection stresses. Set panels level  and plumb to correct positions. Securely brace panels and anchor in place  to maintain plumb until permanently secured by finished structure.

a.	Do not load floors or roof with equipment or materials that exceed  design capacity of the structure without approval of SEOR.

Fit mass timber panels closely and accurately, without trimming, cutting  or other modifications.

a.	Site cutting or boring of panels, other than shown in reviewed shop  drawings is not permitted without written consent of SEOR and AOR.

Join mass timber panels along edges using joint connection indicated in  structural construction drawings.

- Gap between adjacent mass timber panels: Minimum [1/8-inch]<other  value> on all sides.

************************************************************************** NOTE:	Retain the following article if stain and/or

coatings are to be field-applied. The preparation  and finishing requirements will depend on the mass  timber product and field finish to be provided.

Modify the following as appropriate for the end  application and recommendations from the mass timber  panel and finish material manufacturers.

**************************************************************************

# [3.6	FIELD-FINISHING

Preparation: Finish exposed surfaces to remove planning or surfacing marks and to provide a finish equivalent to that produced by machine sanding with No. 120 grit sandpaper.

Field-Finishing:[ Stain][ and] Seal in accordance with Section [09 91 00  PAINTING] [09 93 00 STAINING AND TRANSPARENT FINISHING] [09 96 00

# HIGH-PERFORMANCE COATINGS].

- Applications: Finish occurs at the following locations:

  - [All exterior exposed conditions.]

  - [Interior exposed conditions as indicated.]

# ]3.7	CLEANING

Clean exposed surfaces of mass timber panels after erection and completion  of field touch up.

- Clean all exposed surfaces.

- Perform cleaning procedures, as necessary, according to mass timber  panel manufacturer’s written recommendations and as instructed by AOR.  Protect other work from staining or damage due to cleaning operations.

  - Repair water and rust stains.

- Do not use cleaning materials or processes that could change the  appearance of exposed mass timber panels or damage adjacent materials.

# ADJUSTING

Repair damaged surfaces and finishes of mass timber panels following  erection. Replace damaged mass timber panels if repairs are not approved  by AOR[ SEOR][ and][ SSEOR].

# PROTECTION

After installation, cover each panel with temporary waterproof protection to maintain the low moisture content of the wood. Protect panels against excessive and repeated water deposits and standing water at all times.

Maintain protection until members are enclosed within the building and final coats are ready for application.	Take precautions to closely maintain the manufacturer's standard for moisture content.	Elevate initial building heating/cooling gradually to the desired level.	Do not reduce the relative humidity of the building rapidly.

Protect installed mass timber panels from damage during construction,  including protection in accordance with Contractor’s Weather and Moisture  Protection Plan.

    - Prevent standing water on mass timber panels faces.

    - Adhere to Contractor’s Weather and Moisture Protection Plan for  retention of wrappings on mass timber panels until immediately prior  to installation.

    - Slit underside of wrapping to prevent accumulation of moisture inside  wrapping.

-- End of Section --